## Slide 1: Mapping the impact of temperature and salinity on EOR polyacrylamide performance in reservoir and in produced water treatment
Leena Nurmi, Luciana Bava, Mehrdad Hesampour, Sirkku Hanski
luciana.bava@kemira.com
erica.pin@kemira.com

## Slide 2: Table of content
Introduction
Objectives
Materials
Results – Contour maps
Conclusions

## Slide 3: Introduction
Anionic polyacrylamides are widely used in polymer flooding
Selection of optimal chemical composition of polyacrylamide based on:
  Reservoir and water treatment conditions both considered
  Temperature, salinity, hardness
  Copolymers of acrylic acid and acrylamide (HPAM) for moderate conditions
    Temperature below 50-60°C or low salinity or low hardness
  ATBS (sulfonation) can be added for harsher conditions
Acrylamide
Acrylic acid
ATBS

## Slide 4: Introduction
Acrylic acid (AA)  multivalent cations in brine detrimental for viscosity yield
Hydrolysis reaction takes place above 50-60°C
  Acrylamide (AM) and ATBS  Acrylic acid (AA)
  Rate of hydrolysis highly dependent on reservoir temperature, quite independent on brine composition
Cloud point: AA tolerates multivalent cations better at low temperature  solubility is lost (precipitation) at high temperature
  Cloud point dependent on polymer and brine composition
  Precipitation can occur
ATBS helps
  Slower hydrolysis rate
  Less interaction with multivalent cations

## Slide 5: Key messages
Data collected for optimal polyacrylamide selection
Systematic results provided to predict performance over a range of products and conditions (TDS 700 - 170 000 ppm, T up to 90°C):
Initial viscosity yield
  Important at low or moderate reservoir temperature (up to 50-60°C) where stable viscosity expected
Cloud point
  Exceeding polymer cloud point can bring challenges​ at produced water treatment
  Precipitation on hot heat exchanger surfaces  deposits
  Deposit challenges can be mitigated with polyacrylamide sample selection
Thermal stability
  Important at high reservoir temperature (above 50-60°C) where hydrolysis rate significant

## Slide 6: Polymer samples
Polymer | Acrylamide mol% | Acrylic acid mol% | ATBS mol% | Viscosity [cP] 1 mol/kg NaCl 1000 ppm, 25°C, 7.34 1/s
HPAM-20 | 70 | 20 | 0 | 10.8
HPAM-25 | 75 | 25 | 0 | 12.1 (MW > 15 MDa)
HPAM-33 | 67 | 33 | 0 | 11.0
TER-20-5 | 75 | 20 | 5 | 10.5
TER-20-10 | 70 | 20 | 10 | 10.1
ATBS-15 | 85 | 0 | 15 | 10.6
ATBS-25 | 75 | 0 | 25 | 9.4
Acrylamide
Acrylic acid
ATBS
High molecular weight, typical EOR grades

## Slide 7: Salinity maps
21 artifical brines
Na+, Ca2+, Cl- ions
TDS 730 – 170 000 ppm
Ca2+ ions 0 – 10 400 ppm

## Slide 8: Salinity maps
21 artifical brines
Na+, Ca2+, Cl- ions
TDS 730 – 170 000 ppm
Ca2+ ions 0 – 10 400 ppm
Relative hardness 0 – 20 mol%
Relative hardness [mol%] =
Multivalent cations [mol] (Ca2+, Mg2+,…)
All cations [mol]

## Slide 9: Viscosity yield
HPAM-33, 60°C, 7.34 1/s
Viscosity yield measured at 1000 ppm polymer concentration
  25°C, 60°C, 90°C
Results shown in the salinity map
Similar maps available for other samples (HPAM, terpolymers, ATBS-copolymers)
  Nurmi et al. 2023, EAGE IOR+

## Slide 10: Viscosity yield
Areas 1-7 in the salinity map show different product candidates as highest viscosity option at 60°C
  Nurmi et al. 2023, EAGE IOR+
In practice, polimer selection is not onlybased on initial viscosity yield
  Thermal stability
  Performance in produced water
  Retention, injectivity etc.
Multiple samples, 60°C

## Slide 11: Cloud point
Temperature at which polymer starts to precipitate out from the brine
Dependent on TDS, hardness and polymer’s chemical composition
Temperature increases

## Slide 12: Cloud point
HPAM-25
Effect of brine composition to HPAM-25 cloud point
At moderate reservoir temperature (50-60°C) good solubility within reservoir expected in all tested brine compositions
  BUT deposit challenges may occur if temperatures above cloud point reached in produced water treatment – e.g. at heat exchangers

## Slide 13: Examples of fouling at heat exchanger
Injection water heat exchanger, Mittal, S. et al. SPE-192943-MS
Outlet plate of a heat exchanger, Zagitov, R. et al. SPE-194689-MS
Polymer reaches the cloud point at the heat exchanger temperatures

## Slide 14: Cloud point
Cloud point related deposit risks in produced water treatment can be mitigated with right selection of injected polymer chemistry
  Applicable mainly at moderate temperatures (below 50-60°C)  polymer chemical composition is expected to be stable from injector to producer
HPAM-25
HPAM-20
TER-20-5

## Slide 15: Cloud point
At high reservoir temperature  Hydrolysis decreases cloud point
  Increased risk for deposits in produced water treatment
  Sulfonation helps
HPAM-25
HPAM-49
HPAM-98
Hydrolysis rate at any temperature:
L.Nurmi et al. SPE-190184-MS

## Slide 16: Thermal stability - Viscosity retention
Important at high reservoir temperature (above 50-60°C)​
How much viscosity [%] is retained after HPAM-25 hydrolysis?
Brine composition has big impact on viscosity retention
Brine composition does not have (major) impact on hydrolysis rate in typical EOR brines.
L.Nurmi et al. EAGE IOR 2019

## Slide 17: Thermal stability - Viscosity retention
Important at high reservoir temperature (above 50-60°C)​
How much viscosity [%] is retained after HPAM-25 hydrolysis?
HPAM-25
HPAM-49
HPAM-98
HPAM-42
100%
Effect of brine composition on thermal stability
Hydrolysis is beneficial at low TDS and hardness

## Slide 18: Summary
Optimal chemical composition of polyacrylamide needs to be selected based on both reservoir and water treatment conditions
Systematic results provided to predict initial viscosity yield over a range of polyacrylamide products and conditions (TDS 700- 170 000 ppm, T up to 90°C)
Effect of brine composition to cloud point shown for a range of polyacrylamide products  exceeding cloud point at produced water treatment can be avoided with careful product selection
Systematic results provided for HPAM to predict thermal stability over a wide range of conditions (TDS 700 - 170 000 ppm, T up to 120°C)

## Slide 19: Thank you